## Slide 1
Santoro L., Putzolu F., Mondillo N.
Maria Boni
&
Dipartimento Scienze della Terra, dell’Ambiente e delle Risorse, DISTAR Università di Napoli, Federico II, Italy
Base metals sulphides and barite (Irish type?) in the Paleozoic of SW Sardinia (Italy): facts and (a lot of) open questions
50 YEARS IRISH-TYPE Zn-Pb DEPOSITS
8-10° September

## Slide 2
50 YEARS IRISH-TYPE Zn-Pb DEPOSITS
8-10° September
Irish deposits consist of limestone- and dolomite-hosted stratabound sphalerite-galena-pyrite and barite orebodies, formed primarily by carbonate replacement during multiple diagenetic stages
They are concentrated near normal faults, often associated with several steps of extensional tectonics during the development of sedimentary basins
Irish deposits s.s. are regarded as hybrids between MVT and SedEx styles of mineralization
Can Sardinian ores be considered as “Irish-type” deposits??

## Slide 3
50 YEARS IRISH-TYPE Zn-Pb DEPOSITS
8-10° September

## Slide 4
Breve di Villa di Chiesa (1327 a.C)
Middle Age mines
50 YEARS IRISH-TYPE Zn-Pb DEPOSITS
8-10° September

## Slide 5
Geological setting and tectonic map
B
“External Zone” Iglesiente-Sulcis District
50 YEARS IRISH-TYPE Zn-Pb DEPOSITS
8-10° September
Iglesiente-Sulcis
District
B
B

## Slide 6
Iglesiente-Sulcis district and old mines
50 YEARS IRISH-TYPE Zn-Pb DEPOSITS
8-10° September

## Slide 7
Sedimentary environment and stratigraphic record
50 YEARS IRISH-TYPE Zn-Pb DEPOSITS
8-10° September
The development of the carbonate platform in the Cambrian of Sardinia follows a multi-stage evolution, including the progression from a terrigenous carbonate ramp or a rimmed shelf attached to an easterly continental area (Nebida Group), to an isolated, subsequently flooded, carbonate platform (Gonnesa Group).
The platform was bordered by slope areas leading to western and eastern basins.
The platform was finally covered by terrigenous sediments deposited in an open marine environment (Iglesias Group).

## Slide 8
Sedimentary environment and stratigraphic record
50 YEARS IRISH-TYPE Zn-Pb DEPOSITS
8-10° September
The main control of the evolution of the Cambrian platform was a strong tensional tectonism, mirrored by abrupt facies changes, and coupled with differences in thicknesses and an abundance of breccias at several stratigraphic levels.
Tensional tectonics
Tensional tectonics

## Slide 9
Lagoonal Limestone
Tidal Dolomite
Tidal Dolomite Microbial mats+Stromatolites
Gonnesa Group – Lower Cambrian
Nebida Group – Lower Cambrian
Sandstone
Archaeoc.+Ooids
50 YEARS IRISH-TYPE Zn-Pb DEPOSITS
8-10° September

## Slide 10
The western slope
Planu Sartu (Buggerru)
Well-bedded limestone and dolomite with chert layers and nodules on the western slope
50 YEARS IRISH-TYPE Zn-Pb DEPOSITS
8-10° September
Planu Sartu (Buggerru)
Mega-breccia on the western slope

## Slide 11
50 YEARS IRISH-TYPE Zn-Pb DEPOSITS
8-10° September
Sedimentary environment and stratigraphic record
Drowned carbonate platform: Iglesias shales (Upper Cambrian-Lower Ordovician)
Bindua

## Slide 12
Genna Luas Iron-rich Gossan
Genna Luas Massive Pyrite body
Massive sulphides mineralization
50 YEARS IRISH-TYPE Zn-Pb DEPOSITS
8-10° September

## Slide 13
Massive sulphides mineralization
Campo Pisano
Massive Melnikovite-Pyrite
Campo Pisano
Folded Pyrite & Sphalerite
50 YEARS IRISH-TYPE Zn-Pb DEPOSITS
8-10° September

## Slide 14
MVT / Irish type (?) ores
Disseminated sphalerite & pyrite in peloidal mudstone
Breccia and replacement ores (sphalerite & galena) with calcite layers and bodies
Galena & barite at the top of Gonnesa Group
MVT / Irish type (?) mineralization
50 YEARS IRISH-TYPE Zn-Pb DEPOSITS
8-10° September

## Slide 15
MVT / Irish type (?) mineralization
Peloidal Mudstone replaced by Yellow Sphalerite & collomorph Melnikovite/Pyrite
San Giovanni Mine
A) Sulphides disseminated and replacing mudstone
50 YEARS IRISH-TYPE Zn-Pb DEPOSITS
8-10° September
0.5 mm
Deformed through
Variscan Orogeny
Sph

## Slide 16
MVT / Irish type (?) mineralization
B) Sulphides replacing limestones and in cement of breccia
Monteponi mine
50 YEARS IRISH-TYPE Zn-Pb DEPOSITS
8-10° September
Dark sphalerite & galena replacing limestone

## Slide 17
MVT / Irish type (?) mineralization
C) Barite & galena at the top of Gonnesa limestones
50 YEARS IRISH-TYPE Zn-Pb DEPOSITS
8-10° September
Microcrystalline barite &
galena replacing limestone; both are strongly deformed
S’Ega S’Acqua mine

## Slide 18
MVT / Irish type (?) mineralization
A+B Several successive ore generations
(1) “Peloidal” yellow sphalerite
San Giovanni mine
(2) Dark sphalerite & galena
(3) Sparry calcite
50 YEARS IRISH-TYPE Zn-Pb DEPOSITS
8-10° September

## Slide 19
Petrographic observations
Campo Pisano mine - Pyrite/Melnikovite
Mlk
Masua mine - Pyrite, Sphalerite, Galena
Sph
Py
Ga
200 µm
200 µm
Masua mine - Pyrite concretions & Sphalerite
Py
Sph
100 µm
Genna Luas mine - Pyrite/Melnikovite
Mlk
Py
200 µm
50 YEARS IRISH-TYPE Zn-Pb DEPOSITS
8-10° September

## Slide 20
Old (1920) geological map of the Iglesias syncline
Ordovician “Sardic” tectonic phase (E-W)
Caledonian “Sardic” deformation phase – “E-W” folds
50 YEARS IRISH-TYPE Zn-Pb DEPOSITS
8-10° September

## Slide 21
Unconformity between Cambrian shales and Ordovician conglomerate. Both are deformed later by Variscan orogeny
50 YEARS IRISH-TYPE Zn-Pb DEPOSITS
8-10° September

## Slide 22
Upper Ordovician Sulcis
Ordovician silicified conglomerate (“Puddinga” AUCT.) (1) with carbonate breccia deposits (2) at the base. Both lithologies are sparingly mineralized with barite and sulphides.
(2)
(2)
(1)
(1)
Bacu Abis
50 YEARS IRISH-TYPE Zn-Pb DEPOSITS
8-10° September

## Slide 23
Old (1920) geological map of the Iglesias syncline
Devono-Carboniferous Variscan tectonic phase (N-S)
Variscan deformation phases
1st Variscan phase:
“E-W” folds overprinting those of the Sardic phase
2nd Variscan phase:
“N-S” folds associated with a penetrative axial plane cleavage
(approximately subvertical and
N-S striking)
50 YEARS IRISH-TYPE Zn-Pb DEPOSITS
8-10° September

## Slide 24
Variscan Deformation
Buggerru – San Nicolo’
Folded and twinned calcite layer
S’Ega S’Acqua – Stretched and deformed
dolomite layers (brown) in grey limestone
50 YEARS IRISH-TYPE Zn-Pb DEPOSITS
8-10° September

## Slide 25
Nebida. Upper Ordovician conglomerate
showing the N-S Variscan cleavage
Nebida. Upper Ordovician carbonate breccia showing the N-S Variscan cleavage
50 YEARS IRISH-TYPE Zn-Pb DEPOSITS
8-10° September
Variscan Deformation

## Slide 26
Monteponi mine - old section of the mineralized bodies aligned along
the main Variscan cleavage (approximately N-S striking)
50 YEARS IRISH-TYPE Zn-Pb DEPOSITS
8-10° September

## Slide 27
Monteponi mine lev.-60 - carbonate-hosted oxidized sulphides aligned along the main Variscan cleavage (approximately N-S striking)
50 YEARS IRISH-TYPE Zn-Pb DEPOSITS
8-10° September

## Slide 28
Calcite bodies associated with sulphides
oriented along the N-S Variscan cleavage
Seddas Moddizzis mine
San Giovanni mine
50 YEARS IRISH-TYPE Zn-Pb DEPOSITS
8-10° September

## Slide 29
(1)
(3)
(2)
(1) “Yellow” sphalerite in limestone
(2) “Peloidal” sphalerite in limestone
(3) Red sphalerite in shale & breccia
The mineralizations are stretched
following the N-S Variscan cleavage
San Giovanni mine. Massa Pozzo 2
San Giovanni mine. Massa Pozzo 3
San Giovanni mine. Contatto W
50 YEARS IRISH-TYPE Zn-Pb DEPOSITS
8-10° September

## Slide 30
2 cm
1 cm
Scalittas mine (Masua) Strongly deformed
Cambrian limestone and sulphides
Planu Sartu mine (Buggerru)
Mineralized and deformed breccia
Scalittas mine (Masua) Strongly deformed breccia
with Cambrian limestone clasts. Sulphides in the matrix
50 YEARS IRISH-TYPE Zn-Pb DEPOSITS
8-10° September

## Slide 31
1 mm
sphalerite
pyrite
Variscan foliation
2 mm
pyrite
sphalerite
sphalerite
galena
calcite
500 µm
Brittle deformation
Boudinage
Microeffects of Variscan tectonics
50 YEARS IRISH-TYPE Zn-Pb DEPOSITS
8-10° September
Pressure
shadows

## Slide 32
Cal
Py
Sph
Pyrite, Sphalerite & twinned Calcite
Py
Sph
Sphalerite & Pyrite oriented along a Variscan fault; Ba-rich Muscovite, Al-rich dioctahedral
Chlorite (dunbassite)
Folded Sphalerite, Al-rich dioctahedral Chlorite
400 µm
Sph
Chl
Sph
Py
Folded Sphalerite & Pyrite
50 YEARS IRISH-TYPE Zn-Pb DEPOSITS
8-10° September

## Slide 33
1920
1995
Old and “less old” maps of Iglesias syncline showing the few limestone outcrops in a sea of brown dolomite
50 YEARS IRISH-TYPE Zn-Pb DEPOSITS
8-10° September

## Slide 34
Nebida Coastal Road
Cambrian Limestone
Fe-rich hydrothermal Dolomite
Post Variscan dolomitization
50 YEARS IRISH-TYPE Zn-Pb DEPOSITS
8-10° September

## Slide 35
Post-Variscan dolomitization (underground exposures)
Fe-rich dolomite is NOT oxidized
and NOT deformed
2 hydrothermal dolomite generations (saddle
dolomite), both following the Variscan cleavage
50 YEARS IRISH-TYPE Zn-Pb DEPOSITS
8-10° September

## Slide 36
Su Zurfuru Skarn Breccia – Garnet, Wollastonite, Hedenbergite, Epidote, Sphalerite, Chalcopyrite
Sideru Boi Skarn – Wollastonite, Andradite, Epidote, Chlorite, Magnetite-Hematite, Chalcopyrite
2 cm
Bor
Sph
Py
200 µm
marble
Skarn from late- to post-Variscan granite intrusions
Filone Morettu Skarn – Pyrite, Sphalerite, Bornite
50 YEARS IRISH-TYPE Zn-Pb DEPOSITS
8-10° September

## Slide 37
Post Variscan mineralization (undeformed)
San Giovanni mine – Ag-rich galena and barite in paleokarst breccia at “Grotta Pisani”
M.Boni
1977
50 YEARS IRISH-TYPE Zn-Pb DEPOSITS
8-10° September

## Slide 38
Underground pillar in the “Scavi Pisani” (San Giovanni mine). Post-Variscan hydrothermal breccia
Galena, pyrite & freibergite
Ga
Py
Frb
500 µm
50 YEARS IRISH-TYPE Zn-Pb DEPOSITS
8-10° September

## Slide 39
Monteponi. Old Pisan Ovens for Silver Ore
3 cm
Internal sediments in paleokarst with barite and black chert. Barega mine
San Giovanni mine
Silver-rich ore in paleokarst: Ag-galena, Ankerite, Calcite.
50 YEARS IRISH-TYPE Zn-Pb DEPOSITS
8-10° September

## Slide 40
Primary sulphides
Secondary nonsulphides “Calamines”
Smithsonite & Hemimorphite
50 YEARS IRISH-TYPE Zn-Pb DEPOSITS
8-10° September

## Slide 41
Conclusions I
The Lower Palaeozoic-hosted mineralization of SW Sardinia can be only partly classified as “Irish-type”.
The massive sulphides in the tidal dolomites at the base of the Gonnesa Group with their abundance of pyrite and Fe-rich sphalerite, might have been deposited syngenetically or during early diagenesis on the sea floor or along active faults/feeder channels (SedEx?).
On the contrary, it is reasonable to consider that a significant part of sulphides as well as barite in the limestone-hosted orebodies formed through replacement of the carbonate host and as breccia filling during several diagenetic and post-diagenetic stages. WHEN?
Sulphides in the cement and matrix of multi-generational breccias are particularly abundant close to the Cambrian platform margins and along several NW-SE tectonic lineaments. This also demonstrates a pristine structural control on the mineralization in specific areas of SW Sardinia.
50 YEARS IRISH-TYPE Zn-Pb DEPOSITS
8-10° September

## Slide 42
Conclusions II
The deposition of post-Variscan ores was also subjected to structural control: the lineaments hosting the veins and paleokarst orebodies were conditioned by the extensional tectonics active at the end of the Variscan orogeny, that lasted throughout the Mesozoic.
The effects of Variscan deformation and low-grade regional metamorphism on the pre-Variscan ores in SW Sardinia include changes in: (a) the geometry of sulphide orebodies, and (b) the mineralogy and textures of the ore and gangue minerals. Major and trace element contents of minerals were probably modified as well.
Strong evidence of tectonic control is bound also to the small Upper Ordovician sulphides/barite deposits, with the Cambrian carbonates acting as structural highs that followed a pattern of already active lineaments.
50 YEARS IRISH-TYPE Zn-Pb DEPOSITS
8-10° September

## Slide 43
50 YEARS IRISH-TYPE Zn-Pb DEPOSITS
8-10° September
THANK YOU