## Slide 1: Irish but not Irish-type
Gerry Stanley
and
Colin J. Andrew
Irish-type Zn-Pb deposits around the world
Galway, September 8th – 10th 2023
Irish but not Irish-type

## Slide 2: Outline
Introduction
Kildare
Abbeytown
MVT vs Irish-type
Conclusion
Irish-type Zn-Pb deposits around the world
Galway, September 8th – 10th 2023
Irish but not Irish-type

## Slide 3
Navan
Galmoy
Lisheen
S’mines
Tynagh
Kildare Zn-Pb deposits
Abbeytown Zn-Pb deposits
Introduction
Kildare
Abbeytown
MVT vs Irish-type
Conclusion
The Irish but not Irish-type Deposits
Irish-type Zn-Pb deposits around the world
Galway, September 8th – 10th 2023
Irish but not Irish-type

## Slide 4
Zinc of Ireland announced an updated resource for Kildare (dated September 8th 2020) :
11.3Mt @ 9.0% Zn + Pb (Inferred)
with thick, high grade zones of mineralization, for example:
19.89m @ 17.64% Zn+Pb at McGregor (Canal Zone)
15.65m @ 11.7% Zn+Pb at Shamrock (Bridge Zone)
Bridge Zone
(“Shamrock”)
Canal Zone
(“McGregor”)
“FC3”
Kildare
Introduction
Abbeytown
MVT vs Irish-type
Conclusion
Kildare Resource
Harberton Bridge
Irish-type Zn-Pb deposits around the world
Galway, September 8th – 10th 2023
Irish but not Irish-type

## Slide 5
ALLENWOOD SOUTH
Kildare
Introduction
Abbeytown
MVT vs Irish-type
Conclusion
Allenwood Beds
Rickardstown Formation
Waulsortian Mudbank
ABC Group
Navan Group
Basal Clastics
Lower Palaeozoic
Kildare District Deposits
Irish-type Zn-Pb deposits around the world
Galway, September 8th – 10th 2023
Irish but not Irish-type

## Slide 6
The Allenwood Formation comprise pale grey, massive shelf limestones and their dolomitized equivalents. It is thought that the Allenwood Formation passes laterally into Calp in the basinal areas.
Rickardstown Formation comprises thinly interbedded nodular crinoidal, cherty micrites, shales and reef-derived conglomerates overlain by a dark grey, fine-grained dolomite with abundant chert.
Kildare District: Stratigraphic Setting
Kildare
Introduction
Abbeytown
MVT vs Irish-type
Conclusion
  Sub-Waulsortian – Kildare Province of Philcox (1984) – twice as thick as the Limerick and North Midlands Provinces, and almost four times as thick as the Dunmore Province.
  Comprises a Navan Beds equivalent; Argillaceous Bioclastic Limestones; and laminated calcarenite; Banded Shale; and some thinner limestones at the top.
Irish-type Zn-Pb deposits around the world
Galway, September 8th – 10th 2023
Irish but not Irish-type

## Slide 7
Extract from GSI 100,000 Sheet 16
Allenwood
Harberton Bridge
Rickardstown
Cloncurry
Clongownagh
Boston Hill
Kildare
Introduction
Abbeytown
MVT vs Irish-type
Conclusion
Regional Geology: Kildare District
Irish-type Zn-Pb deposits around the world
Galway, September 8th – 10th 2023
Irish but not Irish-type

## Slide 8
Fe-Zn-Pb mineralization
Brecciation
Waulsortian isopachytes
Fault
Off bank facies
Kildare
Introduction
Abbeytown
MVT vs Irish-type
Conclusion
Waulsortian isopachytes (after Andrew, 1986)
Irish-type Zn-Pb deposits around the world
Galway, September 8th – 10th 2023
Irish but not Irish-type
Notes: Note the Waulsortian knoll form

## Slide 9
Peloidal skeletal grainstone and oolitic limestones
Crinoidal shaley limestones and occasional cherts
Coalesced and stacked stromatactid micrite mudbanks with a few interbedded shale and crinoidal limestone intervals
“Brown Calp”
“Upper Dolomite”
Laminated dolomitic mudstones and thin bioclastic horizons
Argillaceous Bioclastic Limestones and shales, transitional to Waulsortian in parts
Silty Calcarenites
Rickardstown Clongownagh Cloncurry Harberton Allenwood Prosperous
Lucan Formation
Lucan Formation
Allenwood Beds
Silty Calcarenite
Silty Calcarenite
Upper Dolomite
Waulsortian
Waulsortian
Waulsortian
Waul Eq
Waul Eq
Lam Beds
Argillaceous Bioclastic Limestones
Argillaceous Bioclastic Limestones
“Brown Calp”
More Restricted Environments
Shelf and Open Marine Environments
Vertical scale
Schematic section through Kildare Deposits
(length of section approximately 35km)
Kildare
Introduction
Abbeytown
MVT vs Irish-type
Conclusion
250
500
0
Irish-type Zn-Pb deposits around the world
Galway, September 8th – 10th 2023
Irish but not Irish-type

## Slide 10
Kildare
Introduction
Abbeytown
MVT vs Irish-type
Conclusion
The Allenwood Graben, Faults and Corridor Nomenclature
Irish-type Zn-Pb deposits around the world
Galway, September 8th – 10th 2023
Irish but not Irish-type

## Slide 11
Simplified structural plan at base of Waulsortian showing principal faults and distribution of mineralization within the “McGregor Corridor”.
Kildare
Introduction
Abbeytown
MVT vs Irish-type
Conclusion
Irish-type Zn-Pb deposits around the world
Galway, September 8th – 10th 2023
Irish but not Irish-type

## Slide 12
Canal Zone
Section 276000mE facing East
Upper Allenwood Beds
Lower Allenwood Beds
Upper Waulsortian Transition
Waulsortian Mudbank
Argillaceous Bioclastic Limestone
Clean Calcarenite
Biosparites
Dolomitized Waulsortian
Dolomitized Allenwood Beds
>4% Zn+Pb
Rock Matrix Breccia
Crackle & Precipitate Breccias
Allenwood
Fault Control at Harberton Bridge
Kildare
Introduction
Abbeytown
MVT vs Irish-type
Conclusion
Irish-type Zn-Pb deposits around the world
Galway, September 8th – 10th 2023
Irish but not Irish-type

## Slide 13
Canal Zone
Bridge Zone
0 50 100 150m
0m OD
-400m
-200m
0m OD
-400m
-200m
Kildare
Introduction
Abbeytown
MVT vs Irish-type
Conclusion
Section through Harberton Bridge with holes projected 100m either side of line of section
(Modified from Zinc of Ireland NL Investor Presentation, 24 Sept 2022)
Irish-type Zn-Pb deposits around the world
Galway, September 8th – 10th 2023
Irish but not Irish-type

## Slide 14
Inferred Resource 11.3Mt @ 7.8%Zn, 1.2%Pb.
0 100 200m
-100m
-300m
-200m
-400m
Kildare
Introduction
Abbeytown
MVT vs Irish-type
Conclusion
Mineralization distribution
Irish-type Zn-Pb deposits around the world
Galway, September 8th – 10th 2023
Irish but not Irish-type
ZMI investor presentation
McGregor = Canal; Shamrock = Bridge
>5% Zn+Pb
>10% Zn+Pb

## Slide 15
Kildare
Introduction
Abbeytown
MVT vs Irish-type
Conclusion
Schematic section through Rickardstown
Irish-type Zn-Pb deposits around the world
Galway, September 8th – 10th 2023
Irish but not Irish-type

## Slide 16
Kildare
Introduction
Abbeytown
MVT vs Irish-type
Conclusion
Mineralization
Hole ZB16-002 417m – 437m
Massive sphalerite
MVT style
From ZMI website
Irish-type Zn-Pb deposits around the world
Galway, September 8th – 10th 2023
Irish but not Irish-type

## Slide 17
Kildare
Introduction
Abbeytown
MVT vs Irish-type
Conclusion
Z-4069-003
Mineralization
Irish-type Zn-Pb deposits around the world
Galway, September 8th – 10th 2023
Irish but not Irish-type

## Slide 18
Z-4069-003 (McGregor) drill core showing massive sulphides at ~488m downhole.
Kildare
Introduction
Abbeytown
MVT vs Irish-type
Conclusion
Mineralization
Irish-type Zn-Pb deposits around the world
Galway, September 8th – 10th 2023
Irish but not Irish-type

## Slide 19
Allenwood
Rickardstown
Harberton Bridge
Mineralization
1
cm
Kildare
Introduction
Abbeytown
MVT vs Irish-type
Conclusion
Irish-type Zn-Pb deposits around the world
Galway, September 8th – 10th 2023
Irish but not Irish-type
Notes: Note the Waulsortian knoll form

## Slide 20
Kildare
Introduction
Abbeytown
MVT vs Irish-type
Conclusion
Marcasite and schallenblende in collapse breccia.
HB-98 - 98.9m
Harberton Canal Zone – Massive sulphides
ZMI DDH Z-1046-027
2 cm
Marcasite
HB-42 125.7m
Mineralization
Irish-type Zn-Pb deposits around the world
Galway, September 8th – 10th 2023
Irish but not Irish-type

## Slide 21
Kildare
Introduction
Abbeytown
MVT vs Irish-type
Conclusion
From ZMI website
Shamrock zone
Colloform textures
5-10% Zn
Colloform massive sulphide
<30% Zn
Up to 2% Zn
Irish-type Zn-Pb deposits around the world
Galway, September 8th – 10th 2023
Irish but not Irish-type

## Slide 22
Calcite
Dolomite
Ferroan Dolomite
Barite
Marcasite
Sphalerite
Galena
Bitumen
Zn-Pb
phase
Late
Fe
Marcasite predating schallenblende Ferroan dolomite after marcasite Minor galena with sphalerite Late marcasite with calcite
The paragenesis in the Kildare deposits is simple and schallenblende sphalerite shows little variation in chemistry (Fe only).
Barite is scarce and usually in late marcasite. Sulphosalts are virtually absent.
Modified after Trude & Wilkinson (2001)
Paragenesis
Kildare
Introduction
Abbeytown
MVT vs Irish-type
Conclusion
Irish-type Zn-Pb deposits around the world
Galway, September 8th – 10th 2023
Irish but not Irish-type

## Slide 23
Allenwood Beds
Allenwood Beds
Waulsortian
Mudbank
Waulsortian
Mudbank
Tz WML
Tz WML
Calcarenite Marker
A
B
C
C
C
A
B
C
D
After Emo (1986)
~500m
C
A
B
Rock Matrix Breccias
Precipitate Cemented Breccia
Crackle Breccia
Heterolithic Mud Matrix Breccia
D
Kildare
Introduction
Abbeytown
MVT vs Irish-type
Conclusion
Breccia types
Irish-type Zn-Pb deposits around the world
Galway, September 8th – 10th 2023
Irish but not Irish-type

## Slide 24
Multiple horizons
Base of reef
from ZMI website
Kildare
Introduction
Abbeytown
MVT vs Irish-type
Conclusion
Allenwood graben – ZMI mineralization model
Irish-type Zn-Pb deposits around the world
Galway, September 8th – 10th 2023
Irish but not Irish-type

## Slide 25
Data from multiple sources including Gallagher et al. (1992); Dixon et al. (1986); Anderson et al. (1998).
Kildare
Introduction
Abbeytown
MVT vs Irish-type
Conclusion
Kildare deposits
Irish-type deposits
Sulphur isotopes - 1
Irish-type Zn-Pb deposits around the world
Galway, September 8th – 10th 2023
Irish but not Irish-type

## Slide 26
Bacteriogenic Hydrothermal Seawater SO4
Irish-type deposits
Kildare
Introduction
Abbeytown
MVT vs Irish-type
Conclusion
Sulphur isotopes - 2
Irish-type Zn-Pb deposits around the world
Galway, September 8th – 10th 2023
Irish but not Irish-type
Notes: Additionally the Pb isotope results from Harberton are distinctly different from other Irish deposits

## Slide 27
Fluid inclusions
Homogenization Temperature (oC)
Salinity (wt% NaCl equivalent)
Fields for primary inclusions in deposit sphalerites and carbonates derived from data in Banks & Russell (1992), Everett et al. (1997, 1999), Eyre (1998) and Trude & Wilkinson (2001).
Fields for Silesia and Pine Point from Basuki & Spooner (2002).
Pine Point
Silesia
Harberton Bridge fluid inclusion homogenization temperature data is significantly different from the main Irish-type deposits.
The salinity and lower temperatures are indicative of an evaporitic source and coincident with the values for the classic MVT Districts, such as Silesia and Pine Point
Kildare
Introduction
Abbeytown
MVT vs Irish-type
Conclusion
Irish-type Zn-Pb deposits around the world
Galway, September 8th – 10th 2023
Irish but not Irish-type

## Slide 28
Abbeytown
Introduction
Kildare
MVT vs Irish-type
Conclusion
November 1950 to March 1958 | 
Open Pit | 229,269
Index Bed Workings | 283,732
Lower Orebody 1 (Western Orebody) | 28,515
Total | 537,622t @ 2.6% Zn + 1.1% Pb
January 1959 to September 1961 | 
Index Bed | 268
Lower Orebody 1 (Western Orebody) | 11,145
Lower orebody 2 (Under Index Bed) | 142,170
M Zone | 35,734
Total | 185,537t @ 2.0% Zn + 2.1% Pb
Total mined | 730,831t @ 2.45% Zn + 1.38% Pb
Production
after Kelly, 2007
Irish-type Zn-Pb deposits around the world
Galway, September 8th – 10th 2023
Irish but not Irish-type

## Slide 29
350000mN
340000mN
340000mN
150000mE
170000mE
190000mE
Abbeytown
Introduction
Kildare
MVT vs Irish-type
Conclusion
after Geological Survey Ireland (MacDermot et al., 1996) and Hitzman 1986
Regional geology
Irish-type Zn-Pb deposits around the world
Galway, September 8th – 10th 2023
Irish but not Irish-type

## Slide 30
Abbeytown Lmst Mbr
Twigspark Formation
Bundoran Shale
Mullaghmore Sandstone
Benbulben Shale
Glencar and Dartry Limestones
Meenymore Formation
Ballyshannon Limestone
Abbeytown
Introduction
Kildare
MVT vs Irish-type
Conclusion
Stratigraphy
Irish-type Zn-Pb deposits around the world
Galway, September 8th – 10th 2023
Irish but not Irish-type

## Slide 31
Abbeytown
Introduction
Kildare
MVT vs Irish-type
Conclusion
Mine geology
Irish-type Zn-Pb deposits around the world
Galway, September 8th – 10th 2023
Irish but not Irish-type
LOB 1
LOB 2
(Index workings)
M zone
after Hitzman, 1986

## Slide 32
Abbeytown
Introduction
Kildare
MVT vs Irish-type
Conclusion
Mine workings
From Erris Resources website
Irish-type Zn-Pb deposits around the world
Galway, September 8th – 10th 2023
Irish but not Irish-type
after Kelly, 2007

## Slide 33
after Hitzman (1986) and Persellin (2009)
Abbeytown
Introduction
Kildare
MVT vs Irish-type
Conclusion
Mine section
Irish-type Zn-Pb deposits around the world
Galway, September 8th – 10th 2023
Irish but not Irish-type

## Slide 34
Galena rich boulders from Western Workings
Crystalline sphalerite on dolomitized and brecciated host
Abbeytown
Introduction
Kildare
MVT vs Irish-type
Conclusion
Mineralization
Irish-type Zn-Pb deposits around the world
Galway, September 8th – 10th 2023
Irish but not Irish-type

## Slide 35
Abbeytown
Introduction
Kildare
MVT vs Irish-type
Conclusion
Index Bed mineralization
photo by Persellin
Irish-type Zn-Pb deposits around the world
Galway, September 8th – 10th 2023
Irish but not Irish-type

## Slide 36
Abbeytown
Introduction
Kildare
MVT vs Irish-type
Conclusion
C)
D)
Dolomite cements
Large white saddle dolomite (left) and small grey dolomite rhombs (right)
Large, white-brown ferroan saddle dolomite with white calcite
Hydrocarbons
On calcite
On calcite
(after Persellin, 2009)
Dolomite and Hydrocarbons
Irish-type Zn-Pb deposits around the world
Galway, September 8th – 10th 2023
Irish but not Irish-type

## Slide 37
Abbeytown
Introduction
Kildare
MVT vs Irish-type
Conclusion
Paragenesis
Irish-type Zn-Pb deposits around the world
Galway, September 8th – 10th 2023
Irish but not Irish-type
after Hitzman, 1986

## Slide 38
Abbeytown
Introduction
Kildare
MVT vs Irish-type
Conclusion
Fluid inclusions
Irish-type Zn-Pb deposits around the world
Galway, September 8th – 10th 2023
Irish but not Irish-type
after Persellin, 2009

## Slide 39
MVT vs Irish-type
Introduction
Kildare
Abbeytown
Conclusion
Deposit morphology
Irish-type Zn-Pb deposits around the world
Galway, September 8th – 10th 2023
Irish but not Irish-type

## Slide 40
Robb Lake, after Paradis (1999)
Pine Point, from Osisko Metals Inc website
East Tennessee, after Leach and Sangster (1993)
~400m
~60m
Irish-type Zn-Pb deposits around the world
Galway, September 8th – 10th 2023
Irish but not Irish-type

## Slide 41
MVT vs Irish-type
Introduction
Kildare
Abbeytown
Conclusion
Mineral textures
Gordonsville, Central Tennessee
Irish-type Zn-Pb deposits around the world
Galway, September 8th – 10th 2023
Irish but not Irish-type

## Slide 42
MVT vs Irish-type
Introduction
Kildare
Abbeytown
Conclusion
Mineral textures
(Kildare and Abbeytown)
1
cm
Irish-type Zn-Pb deposits around the world
Galway, September 8th – 10th 2023
Irish but not Irish-type

## Slide 43
MVT vs Irish-type
Introduction
Kildare
Abbeytown
Conclusion
Mineral textures
(MVT deposits from around the world)
Pine Point, NWT
Robb Lake, British Columbia
Crackle breccia
Rubble breccia
Mosaic breccia
Rock matrix breccia
Cadjebut, Western Australia
20cm
1cm
Polaris, Nunavut
Irish-type Zn-Pb deposits around the world
Galway, September 8th – 10th 2023
Irish but not Irish-type

## Slide 44
Upper Silesia, Poland
Lucky Dog, Arkansas
Gordonsville, Tennessee
Pomorzany
Trzebionka
Trzebionka
Mineral textures
(MVT deposits from around the world)
Irish-type Zn-Pb deposits around the world
Galway, September 8th – 10th 2023
Irish but not Irish-type
Nanisivik, Nunavut

## Slide 45
Buick, Viburnum, Missouri
Reocin, Spain
Mineral textures
(MVT deposits from around the world)
Irish-type Zn-Pb deposits around the world
Galway, September 8th – 10th 2023
Irish but not Irish-type

## Slide 46
Colloform textures
Zebra textures
Pomorzany
Olkusz
Daniel’s Harbour, Newfoundland
Cadjebut, Western Australia
Other MVT Textures
Irish-type Zn-Pb deposits around the world
Galway, September 8th – 10th 2023
Irish but not Irish-type

## Slide 47
MVT vs Irish-type
Introduction
Kildare
Abbeytown
Conclusion
Sulphur isotopes
Bacteriogenic Hydrothermal Seawater SO4
Irish-type deposits
Sulphur isotopes
Irish-type Zn-Pb deposits around the world
Galway, September 8th – 10th 2023
Irish but not Irish-type

## Slide 48
MVT vs Irish-type
Introduction
Kildare
Abbeytown
Conclusion
Age and timing of mineralization
Kildare
Hosted in late Chadian to early Arundian sedimentary rocks
Cut by NW-SE late faults which also displaces the Kildare Thrust which is of Variscan age (~310Ma)
Therefore, the mineralization must be post Variscan
Abbeytown
Hosted by Chadian sedimentary rocks
Post initial onset of movement (Asbian) on the faults associated with the up-lift of the Ox Mountains Inlier
Hitzman (1986) - Asbian or later age based on the structural history of the area
Halliday and Mitchell (1983) - Permian age based on K-Ar dating (270 and 285Ma) of chlorite intergrown with sphalerite and galena
Irish-type Zn-Pb deposits around the world
Galway, September 8th – 10th 2023
Irish but not Irish-type

## Slide 49
Hosted by rocks younger than typical Irish-type deposits: Kildare deposits are developed over a stratigraphic interval of around 500m into post-Chadian sedimentary rocks. Abbeytown hosted by Chadian rocks.
Isotopically very different, notably with no bacteriogenic sulphur (in marked contrast to all Irish-type deposits) – evaporitic sulphur source likely.
Abundant marcasite in Kildare rather than pyrite as at the Irish-type deposits.
Simple paragenesis with limited phases.
Fluid inclusions: - 45-70°C, 12-17wt% NaCl equivalent (lower T).
Evidence suggests that both the Kildare and Abbeytown deposits are younger than Irish-type deposits.
MVT vs Irish-type
Introduction
Kildare
Abbeytown
Conclusion
Main differences with Irish-type deposits
Irish-type Zn-Pb deposits around the world
Galway, September 8th – 10th 2023
Irish but not Irish-type

## Slide 50
The term ‘‘Irish-type’’ should be reserved for deposits that display the criteria usually associated with such deposits.
The Kildare and Abbeytown deposits have features that do not occur in Irish-type deposits.
The deposits in Kildare and at Abbeytown display many features that are typical of Mississippi Valley-type deposits.
However, the deposits in Kildare and at Abbeytown represent an end-member of the spectrum of mineral deposits observed in the Irish Orefield – they are Irish but not Irish-type.
Conclusion
Introduction
Kildare
Abbeytown
MVT vs Irish-type
Conclusion
Irish-type Zn-Pb deposits around the world
Galway, September 8th – 10th 2023
Irish but not Irish-type